## Slide 1: MFront User Meeting 2024 Micromechanical modelling of closed-cell foams under compression by coupling FEniCS with MFront
L. Liu1, F. Liu1, D. Zenkert2, M. Åkermo2, M. Fagerström1
1Chalmers University of Technology, Sweden 2KTH Royal Institute of Technology, Sweden
Email address: l.liu@chalmers.se
Notes: Reveal the underlying mechanisms, with the power of coupling

## Slide 2: Introduction
  Closed-cell foams
  Excellent mechanical properties
    Low density
    High stiffness and strength
    Energy absorption
    Acoustic isolation
Polymer foam market (in Billion)
www.precedenceresearch.com
www.amiplastics.com
www.sportsdirect.com
www.soniflex.com
Notes: A bit on background
Still growing

## Slide 3
  Underlying mesostructures
    Large number of cells
    Thin cell walls
    Cell shape anisotropy
Aluminium
PVC
PIR
Foam rise
Tang et al., 2022
Mu et al., 2010
Andersons et al., 2010
PVC foam compression
Strain [-]
Stress [MPa]
Shafiq et al., 2015
Notes: For load-bearing applications, compressive behaviour

## Slide 4
  What are the key deformation mechanisms governing the anisotropic compressive behaviour?
Notes: To date, not fully understood, low-density foams

## Slide 5: RVE problem description
  Finite rotation shell formulation
  Kinematics
  Stress resultants
Campello et al., 2003
with
with
Notes: Single cell is sketched as an example
Paramertized
From initial to current
Constitutive, back-rotated
Details

## Slide 6
  Mixed stress-strain driven formulation
  Classical homogenization for mesoscale shell problem
  Weak form
Notes: RVE problem, specific stress state
Classical homogenization, Hill-Mandel
Decompose
Resulting weak form, P appears like

## Slide 7: Quan. method of cell wall behaviour
  Strain energy partitioning indicator
  Membrane energy
  Bending energy
  Time
  0
  Time
  -1
  1
  Buckling occurrence detector
  Partitioning indicator rate
Notes: To identify
Low-density

## Slide 8: RVE simulation setup
  Geometrical model configurations
  Divinycell foam grade H100
    Mesostructural stochastics
Neper
+
Parameter | Symbol | H100
RVE dimension 1 | L1 | 1.5 [mm]
RVE dimension 2 | L2 | 1.5 [mm]
RVE dimension 2 | L3 | 1.5 [mm]
Cell shape anisotropy | R | 1.2 [-]
Cell equivalent diameter | (µd,σd) | (0.35,0.10) [mm]
Cell wall thickness | (µt,σt) | (0.0115,0.0059) [mm]
Nominal relative density | ρ/ρr | 0.0714 [-]
Zhou et al., 2023
Complexity
Notes: H100 as an example, global directions
A side study, fewer stochastics

## Slide 9
  Material model
  Finite-strain isotropic elasticity for shell problem
  Boundary conditions and loads
  Fully prescribed boundary conditions
  Uniaxial compression
+
with
Parameter | Symbol | PVC
Young’s modulus | E | 2700 [MPa]
Poisson’s ratio | ν | 0.38 [-]
Zhou et al., 2023
Disp. fluctuations
Notes: Have not yet managed, explain why later, sufficient for low-density foams upon failure
Fluctuations are supressed
Unprescribed, non-diagonal also prescribed

## Slide 10
  Implementation
  MFront
@DSL DefaultGenericBehaviour;
@Behaviour finiteRotationElasticityShellLF;
@ModellingHypothesis PlaneStress;
// Specify the generalized strains and stresses
@Gradient DeformationGradientTensor Fmm;
Fmm.setEntryName("MembraneDeformationGradient");
…
// Specify the tangent stiffness
@TangentOperatorBlocks{∂Nmm∕∂ΔFmm, ∂Nss∕∂Δess, ∂Mbb∕∂Δkbb, ∂Ndd∕∂Δedd};
// Specify the material parameters
@MaterialProperty stress E;
E.setGlossaryName("YoungModulus");
@MaterialProperty real nu;
nu.setGlossaryName("PoissonRatio");
…
// Specify the internal variables
@StateVariable length th;
th.setEntryName("Thickness");
// Specify the local variables
@LocalVariable stress lambda;
@LocalVariable stress mu;
…
// Initialize several local variables
@InitLocalVariables{
lambda = computeLambda(E,nu);
mu = computeMu(E,nu);
…
}
// Compute the stresses
@Integrator{
// Specific treatment due to plane stress
Fmm(2) = 1.;
const auto Fmm1 = eval(Fmm + ΔFmm);
const auto emm = computeGreenLagrangeTensor(Fmm1);
Smm = th*(lambda_ps*trace(emm)*Stensor::Id()+2.*mu*emm);
Nmm = Fmm1 * Smm;
…
}
// Compute the tangent stiffness
@TangentOperator{
static_cast<void>(smt);
const auto Delmm = th*(lambda_ps*Stensor4::IxI()+2.*mu*Stensor4::Id());
…
∂Nmm∕∂ΔFmm = convert<FiniteStrainBehaviourTangentOperatorBase::DPK1_DF,
FiniteStrainBehaviourTangentOperatorBase::DS_DEGL>(Delmm, Fmm, Fmm1, σmm);
…
}

## Slide 11
  FEniCS
import mgis.behaviour as mgis_bv
…
from rotation_parametrization import ExponentialMap
…
# Specify the modelling hypothesis
hp = mgis_bv.Hypothesis.PlaneStress
# Load the defined material behaviour file
bv = mgis_bv.load('src/libBehaviour.so','finiteRotationElasticityShellLF',hp)
# Set up the material data manager
mat = mgis_bv.MaterialDataManager(bv, ngs)
…
for s in [mat.s0, mat.s1]:
mgis_bv.setMaterialProperty(s, "YoungModulus", E)
…
# Upload the initial strains to the material data manager
mat.s1.gradients[:, 0:5] = Fmm.vector().get_local().reshape((mat.n, 5))
…
# Integrate the material behaviour
it = mgis_bv.IntegrationType.IntegrationWithConsistentTangentOperator
mgis_bv.integrate(mat, it, 0, 0, mat.n)
# Download the initial stresses and tangent stiffness from the material data manager
Nmm.vector().set_local(mat.s1.thermodynamic_forces[:, 0:5].flatten())
Nmm.vector().apply("insert")
…
Ctmm.vector().set_local(mat.K[:,0:25].flatten())
Ctmm.vector().apply("insert")
…
# Upload the current strains to the material data manager
mat.s1.gradients[:, 0:5] = Fmm.vector().get_local().reshape((mat.n, 5))
…
# Integrate the material behaviour
it = mgis_bv.IntegrationType.IntegrationWithConsistentTangentOperator
mgis_bv.integrate(mat, it, 0, 0, mat.n)
# Download the current stresses and tangent stiffness from the material data manager
Nmm.vector().set_local(mat.s1.thermodynamic_forces[:, 0:5].flatten())
Nmm.vector().apply("insert")
…
Ctmm.vector().set_local(mat.K[:,0:25].flatten())
Ctmm.vector().apply("insert")
…
Numerical tours of continuum mechanics using FEniCS
comet-fenics.readthedocs.io
Notes: Register

## Slide 12: RVE simulation results
  Effective responses under compression
Stress
Strain energy fractions
Notes: Global directions
Apparently higher, anisotropic, plateau region is absent
Membrane mode dominates, bending after stiffness reduction

## Slide 13
  Cell wall behaviour
Transverse
Foam rise
Notes: To rationalize
Most cell walls deform first by stretching

## Slide 14
  Effective compressive properties
Transverse
Foam rise
Model set | Cell size | Cell wall thickness
StSt | Stochastics | Stochastics
StCt | Stochastics | Constant
CtCt | Constant | Constant
Complexity
Complexity
Notes: Experimental data as a reference
With different, great agreement
Modulus, strength
Poisson’s ratio

## Slide 15: Conclusions
  Deformation mechanisms
  Cell wall stretching dominates the initial elastic region
  Bending gets crucial only after failure
  Mesostructural stochastics
  Important to be accounted for
  More stochastics result in lower strength
Thanks to the customization and flexibility of FEniCS and MFront!
+

## Slide 16: Ongoing work
  Finite-strain isotropic elasto-plasticity for shell problem
  Ilyushin-Shapiro two-surface yield function
    Membrane state (1)
    Bending state (2)
  Implementation through MFront
  Not fully understood
  Documentation
Dujc et al., 2012
Notes: Examples, trial and error, not efficient
Syntax and possible operations, transpose and inverse
Documentation, only French one

## Slide 17: Logotype
Thank you!
Questions?